Section

Aluminum Cornice Specifications

Part 1 – General

1.01	Summary

A.	Provide aluminum cornice work shown on the drawings, as specified herein, and as needed for a complete and proper installation.

B.	Coordinate cornice work of this section with General Conditions and Supplementary Conditions.

1.02	Submittals

A.	Submit shop drawings in accordance with drawing requirements.

B.	Submit physical sample of cornice profile as based on approved shop 			drawings.

C.	Submit color samples of stock colors.

1.03	Quality Assurance

A.	Use materials which shall be free from defects impairing strength, durability, and appearance; shall be of best commercial quality for purpose required; and shall comply with approved drawings.

B.	Use manufacturer who has had over fifteen (15) years of experience in professional cornice design and fabrication.

1.04	Warranty

A.  	Warrant the product provided for one year after date of delivery of product installed by others.

Part 2 – Products

2.01	Manufacturer

A.	Use aluminum cornice as manufactured by:

Décor Architectural Products, Inc.

2375 Dorr Street Suite E, Toledo, OH 43607

Phone: 419-537-9493, Fax: 419-537-9493

Email: decorap@sbcglobal.net.

2.02	Materials

A.	Use aluminum sheets – alloy 3003, Temper H-14 with available stock finishes.

2.03	Fabrication

A.	Cornice fascia and trim shop formed true to profile as shown in accordance to approved drawings.

B.	Furnish in maximum 10’-0” lengths

D.	Corners and peaks to be shop mitered, formed and assembled.

E.	Joints to be built-in expansion/contraction joints consisting of a special backer plate, shop laminated to one end of the cornice.  Joints to lap approx. 1”.  Lapped cornice should be able to float freely.

F.	Cornice shall have a ½”urethane board laminated to the back side of the aluminum, as needed, to reduce “oil canning”.

2.04	Finishes

A.	Use either -- .032 Aluminum baked on polyester finish

Or -- .032, .040, .050 Aluminum Kynar 500 finishes

B.	Color to be selected from manufacturer standard colors

2.05	Accessories

A.	Design, fabricate, and manufacture cornice moldings in accordance with approved drawings.

B.	Special cornice moldings to be shop painted – attached in accordance with good, acceptable practices in accordance with approved drawings.

Part 3 – Execution

3.01	Project Site Conditions

A.	Verify that site conditions are suitable and accessible for delivery and installation.

B.	Confirm that all preparatory work is in place in accordance with approved shop drawings before delivery and installation.

C.	Provide for proper storage after delivery of cornice.

3.02	Installation

A.	Cornice System – The entire installation of the cornice system shall be in accordance with the manufacturer’s shop drawings.

B.	Expansion Provisions:  Install running lengths to allow controlled expansion for movement of metal components in relation not only to one another but also to adjoining dissimilar materials, including flashing and roofing membrane materials, in a manner sufficient to prevent water leakage, deformation, or damage.  Lap joints a minimum of 1”

End of Section